## Slide 1: MicroLap Technology
Depth Profiling of Composition
Some samples are too opaque to allow the IR beam to penetrate to the depth of interest. Spectral overlaps may also interfere with depth profiling.
In these cases a micro-lapping approach allows spectra to be measured layer-by-layer.
In other cases micro-lapping can be used to calibrate PAS non destructive depth profiling during methods development.

## Slide 2: Depth Profiling Using the MicroLap Process
1. Measure Thickness
2. Measure Spectrum
3. Lap off a Layer
4. Repeat layer by Layer

## Slide 3: MTEC MicroLapper and Thickness Gage
Notes: Microlap.jpg

## Slide 4
Lapping Puck
Ball Joint
Puck
Adhesive
Polymer Layers
or Gradient
Lapped
Surface
10 mm
Sample

## Slide 5
Lapper Motion
Loading
Mass
Rotating
Micro-Abrasive
Ball Joint
Rotating
Puck
Timer
Blow-off Jet
Oscillating Lapper Arm

## Slide 6
0
10
50
60
70
80
20
30
40
PolyProp
Transition
PolyProp
EVOH
Successive Spectra Measured as a Function of Depth

## Slide 7: PAS Analysis of Composite Scorching
Scorching occurs when jet exhaust strikes nearby aircraft (navy carrier decks).
Carbon fiber/BMI panel scorched with air stream at 617 °C for 15 seconds. No visible change.
PA spectra taken as material removed by microlapping.
Notes: 7
Microlapper Transparent.gif

## Slide 8: PA Spectra Taken During Microlapping of Scorched Area
Notes: 8
Depth Profiling Scorched Composite 2.jnb; Spectra at Various Depths graph

## Slide 9: Peak Height Ratios versus Depth into Scorch
Damaged Transition Undamaged
Notes: 9
Scorched Composite Peaks Ratio.gif (from Depth Profiling Scorched Composite 2.jnb)

## Slide 10: Additional Information Can Be Found in the MTEC Applications Library:
Microlap Depth Profiling of a Paper Coating
MicroLap Depth Profiling of Automobile Paint Weathering
Quantitative Depth Profiling Saturation-Equalized Photoacoustic Spectra